| Programme: | IDEI |
| --- | --- |
| Project type: | Exploratory Research Projects |
| Project: | PCE_2012-4-0261 |
| Contact No. | 53/02.09.2013 |
| Project name: | New coordination networks containing polyfunctional flexible bridges |

Scientific Report

2015

Objectives:

1.Preparation of the extended networks containing metals by using the obtained ligands (continued)

1.1.Preparation of networks based on flexible organosilicon ligands and metal salts.

1.2.Determining the chemical and structural composition of the obtained metal complexes by using physical methods of analysis: elemental analysis, TGA, FTIR (MIR/FIR), EDXRF, XRD

1.3.Selection of the interest structures and their investigation by SEM, TEM, AFM to evaluate the morphology and porosity; study of the surface properties by DVS.

2. Preparation of the extended networks based on preformed or in situ clusters and the obtained ligands

2.1. Preparation of networks based on flexible ligands and different metallic precursors

2.2. Determining the chemical composition and the structure of the obtained metal complexes by using physical methods of analysis: elemental analysis, TGA, FTIR (MIR/FIR), EDXRF, XRD and single crystal X-ray diffraction.

2.3. Selection of the interest structures and their investigation by SEM, TEM, AFM to evaluate the morphology and porosity; study of the surface properties by DVS.

Expected results:

At least a novel metallo-silicon network – achieved objective

Seven new metallo-silicon networks based on carboxylic acid and Schiff base ligands synthesized in the previous stages of the project and metal ions of the transition metals were obtained. Their structures were confirmed by elemental analysis, spectral methods (FTIR, UV-vis, ESI-MS) and by single crystal X-ray diffraction analysis.The evaluation of the thermal, morphological and surface properties of the prepared metallo-silicon networks was done by specific methods: thermogravimetrical analysis, AFM, SEM, TEM, EDXRF.

At least a novel network containing metallic clusters and flexible bridges – achieved objective.

Seven novel structures containing metallic clusters and flexible (siloxane and/or alkyl) bridges were obtained on the basis of metal ions and carboxylic acids and Schiff base ligands synthesized in the previous stages of the project.Their structures were confirmed by elemental analysis, spectral methods (FTIR, UV-vis, ESI-MS) and by single crystal X-ray diffraction analysis.The evaluation of the thermal, morphological and surface properties of the prepared metallo-silicon networks was done by specific methods: thermogravimetrical analysis, AFM, SEM, TEM, EDXRF.

At least two presentation at scientific meetings- achieved objective.

The results of the research carried out in this stage of the project have been presented at national and international scientific events in the form of oral presentations (11) and posters (5).

At least two scientific articles submitted at ISI journals-achieved objective.

The results obtained in this stage of the project have been published in ISI journals, their number being larger than expected, 11 being published.

Scientific reportachieved objective.

Table including some of the synthesized compounds in this stage of the project

| No. | Compounds/structure type | Confirmation and investigation methods |  | Remarks |  |
| --- | --- | --- | --- | --- | --- |
| Objective 1. Preparation of the extended networks containing metals by using the obtained ligands (continued) Expected indicator: at least a novel metallo-silicon network;Achieved: 7 |  |  |  |  |  |
| 1. | XRD structure of the coordination network {[Zn2(COO)4(DMF)2]·0.8DMF}n IR max (KBr), cm-1: 3431w, 3067w, 3049w, 2930w, 1676s, 1624vs, 1543m, 1497s, 1410, 1383s, 1254m, 1190m, 1107w, 1063w, 1001w, 845m, 773vs, 723m, 706m, 635m, 540w, 509w, 476vw, 430vw, 384vw. Anal.Calcd. for C60.4H55.6N2.8O10.8Si2Zn2 (Mr 1180.4 g/mol): C, 61.41 %; H, 4.71 %; N, 3.32 %. Found: C 61.28 %; H 4.72 %; N 3.29 %. FTIR spectrum and TG/DTG curves of the coordination polymer {[Zn2(COO)4(DMF)2]·0.8DMF}n | FTIR Elemental analysis UV-vis XRD TG/DTG DSC DVS |  | Indicator of achievement |  |
| 2. | XRD structure of the coordination network [CuL2]n IR max (KBr), cm-1: 3443w, 3059vw, 3042vw, 2955m, 2920m, 2903m, 2855w, 1711vs, 1655m, 1622vs, 1589vs, 1543vs, 1501m, 1450s, 1396s, 1344m, 1313vs, 1306vs, 1248vs, 1198s, 1173s, 1109s, 1082m, 1018m, 988w, 974m, 856vs, 766s, 739m, 702m, 669w, 625w, 559w, 496m, 419w, 397w. Anal. Calcd. for: C42H48N2O8Si2CuCl4 (Mr=970,3772 g-mol): C, 51.98; H, 4.98; N, 3.71. Found C, 52.24; H, 4.81; N, 3.73. ESI-MS: m/z 637 [Cu(HL2)]2+ și m/z 1561 [M + H]+. Sorption/desorption isotherms and TEM image of the coordination polymer [CuL2]n | FTIR Elemental analysis ESI-MS UV-vis XRD TG/DTG DSC DVS TEM |  | Indicator of achievement |  |
| 3. | Dimeric associate in the crystal network of the complex [Zn(L)2] IR max (KBr), cm-1: 3387w, 3076vw, 2951m, 2891m, 1699vs, 1612s, 1599vs, 1568s, 1541m, 1506w, 1491m, 1468m, 1447m, 1414m, 1379m, 1350vw, 1319s, 1279vs, 1246s, 1180s, 1150s, 1126s, 1113s, 1063w, 1030w, 1015w, 991w, 961m, 912m, 856s, 839vs, 772s, 758s, 694s, 636w, 600w, 590w, 582w, 561vw, 526w, 517w, 492w, 447w, 405w. ESI-MS: m/z 774.3 ([Zn(L)2]), 797.2 ([Zn(L)2 + Na]+) Anal. Calcd. for: C40H48N2O6Si2Zn (Mr 774.35 g/mol): C, 62.34; H, 6.28; N, 3.61. Found C, 62.04; H, 6.25; N, 3.62. FTIR and MS spectra of the complex ([Zn(L)2 | FTIR Elemental analysis ESI-MS UV-vis XRD TG/DTG |  | Indicator of achievement |  |
| 4. | View of 3D network in the crystal structure of the complex ZnHL2 IR max (KBr), cm-1: 3377m, 3082vw, 3049vw, 2982vw, 2949m, 2891w, 2847vw, 1693s, 1634vs, 1603s, 1553m, 1501s, 1458m, 1439m, 1429w, 1394w, 1369m, 1346w, 1329m, 1290s, 1248s, 1236s, 1194s, 1169vs, 1126vs, 1113vs, 1072s, 1047s, 1013m, 989vw, 974vw, 959m, 949m, 903w, 868s, 851s, 841s, 787m, 768m, 746s, 735s, 687m, 665w, 623s, 575w, 527m, 496m, 449w, 430w, 417w. Anal. Calcd. for: C42H58N2O18Si2ZnCl2 (Mr 1071.35 g/mol): C, 47.03; H, 5.46; N, 2.61. Found C, 47.41; H, 5.68; N, 2.55. ESI-MS: m/z 834.3 TG and DTG curves of the coordination network [ZnHL2]n | FTIR Elemental analysis ESI-MS UV-vis XRD TG/DTG |  | Indicator of achievement |  |
| 5. | XRD structure of the complex Cu-L IR max (KBr), cm-1:3057vw, 2953m, 1620vs, 1549m, 1472s, 1448s, 1402m, 1329m, 1312m, 1246vs, 1223s, 1198w, 1169m, 1107s, 1082s, 1061s, 970m, 945w, 881w, 839s, 795m, 785m, 741s, 708w, 623m, 565vw, 469w; Anal. Calcd for C26H38CuN2O5Si2 (Mr 578.3 g/mol): C, 55.99; H, 6.62; N, 4.84. Found: C, 56.08; H, 6.68; N, 4.78; ESI-MS: m/z 578.3 ([M]), 596.35 ([M+H2O]) Supramolecular polymeric chain and view of the crystal structure on the crystallographic axis b | FTIR Elemental analysis ESI-MS UV-vis XRD Superficial tension AFM TEM |  | Indicator of achievement |  |
| 6. | XRD structure of the complex Zn-L IR max (KBr), cm-1: 3051w, 3026w, 2947m, 2924m, 2905m, 2878w, 1626vs, 1601s, 1537s, 1468s, 1448vs, 1400s, 1342s, 1319s, 1252s, 1190s, 1163m, 1150s, 1126m, 1078vs, 1026m, 995w, 986w, 912m, 883m, 878m, 853m, 837s, 793s, 777m, 766s, 754s, 741m, 704m, 667w, 636w, 602m, 561w, 546w, 519w, 465m, 451m, 386w; Anal. Calcd for C24H34N2O3Si2Zn (Mr 520.08 g/mol): C, 55.37; H, 6.53; N, 5.38. Found: C, 55.48; H, 6.36; N, 5.39; ESI-MS: m/z 519.44 ([M+]), 541.32 ([M+Na]+), 1039.32 ([2·M+]), 1063.40 ([2·M+Na]+), 1583.72 ([3·M+Na]+). Supramolecular polymeric chain and view of the crystal structure on the crystallographic axis c | FTIR Elemental analysis ESI-MS UV-vis XRD Superficial tension AFM TEM |  | Indicator of achievement |  |
| 7. | XRD molecular structure of ferrocenyl-siloxane uree FSU View of the crystal structure on the crystallographic axis a and supramolecular polymer chain in the crystal structure TEM and STEM images of FSU from chloroform; EDX image of FSU | FTIR Elemental analysis ESI-MS UV-vis 1H-NMR XRD EDX TEM |  | Indicator of achievement |  |
| Objective 2. Preparation of the extended networks based on preformed or in situ clusters and the obtained ligands; Expected indicator: At least a novel network containing metallic clusters and flexible bridges; Achieved: 7. |  |  |  |  |  |
| 1. | Chemical structure of the tetranuclear complex [Cu4(μ4-O)(L1)2Cl4] FTIR (KBr): 3549 (w), 3416 (m), 2951(m), 2918 (m), 2899 (m), 2868 (m), 1634 (vs), 1618 (s), 1562 (vs),1458 (s), 1410 (m), 1385 (m), 1342 (s), 1306 (w), 1288 (w), 1254 (s),1186 (m), 1051 (s), 991 (m), 968 (w), 874 (w), 835 (vs), 797 (s), 777(s), 768 (s), 741 (w), 702 (w), 619 (m), 571 (w), 532 (vw), 509 (m),492 (m) cm–1. UV/Vis (CHCl3): λmax (ε, m–1cm–1) = 375 (19180), 655 (236) nm. MS (ESI+): m/z = 1127 [Cu4(μ4-O)(L1)Cl3]+. Anal. Calc. for C38H62Cl4Cu4N4O5Si4 (1163.3): C 39.23, H 5.37, N 4.81; Found C 39.02, H 5.19, N 4.70. FTIR spectrum and XRD structure of the complex [Cu4(μ4-O)(L1)2Cl4] | FTIR UV-vis Elemental analysis ESI-MS XRD |  | Indicator of achievement |  |
| 2. | Chemical structure of the tetranuclear complex [Cu4(μ4-O)(L2)2Cl4] Anal calc. for C62H74Cl4Cu4N4O11Si4 (1559.6): C 47.75, H 4.78, N 3.59; Found: C 47.67, H 4.64, N 3.62. FTIR (KBr): 3416 (m), 3061 (vw), 2955 (m), 2922 (w), 2903 (w), 1711 (vs), 1624 (vs), 1587 (s), 1543 (vs), 1502 (m), 1420 (m), 1398 (m), 1346 (m), 1315 (vs), 1306 (vs), 1250 (vs), 1196 (m), 1175 (s), 1109 (s), 1082 (s), 1018 (m), 1001 (w), 980 (w), 955 (w), 856 (vs), 766 (s), 702 (m), 663 (vw), 623 (w), 557 (w), 496 (m), 417 (w) cm–1. UV/Vis (CHCl3): λmax (ε, m–1cm–1) = 384 (38300), 415 (38060), 745 (550) nm. MS (ESI+): m/z = 1561 [M + H]+, 637 [Cu(HL2)]2+. FTIR spectrum and XRD structure of the complex Cu4(μ4-O)(L2)2Cl4] | FTIR UV-vis Elemental analysis ESI-MS XRD |  | Indicator of achievement |  |
| 3. | Chemical structure of the dinuclear complex [Co2Cl2L4] IR max (KBr), cm-1: 3425m, 3057vw, 2955m, 2904w, 1714vs, 1636vs, 1599s, 1537vs, 1501m, 1414w, 1388, 1313vs, 1303vs, 1249vs, 1237s, 1198s, 1172s, 1110s, 1071m, 1015m, 1000m, 854vs, 766s, 732w, 701m, 622vw, 602vw, 519w, 395w. Anal. Calc for C124H148Cl6Co3N8O20Si8: C 55.47, H 5.56, N 4.17; Found: C 55.68, H 5.64, N 4.62. ESI-MS: m/z 1204 (1/2 [Co2Cl2L4]). XRD structure of the complex [Co2Cl2L4]·4CH3CN·0.25H2O and the projection of the coordinative node Co2 FTIR spectrum of the complex [Co2Cl2L4] | FTIR UV-vis Elemental analysis ESI-MS XRD |  | Indicator of achievement |  |
| 4. | IR max (KBr), cm-1: 3443w, 3058vw, 2951m, 2893m, 1720vs, 1623s, 1544vs, 1502m, 1447w, 1397m, 1387m, 1347m, 1248s, 1180s, 1105s, 1082, 1017m, 979w, 860vs, 836s, 766w, 696m, 626w, 558w, 497m, 428vw, 385vw. UV/Vis (DMF): λmax (ε, m–1cm–1) = 288 (26154), 412 (10566) nm. Anal. Calc for C70H92.5Cl4Cu4N4O12.75Si4 (Mr 1702.3 g/mol): C 49.39, H 5.48, N 3.29; Found: C 50.08, H 5.61, N 3.62. FTIR and UV-vis spectraof the complex [Cu4(μ4-O)(LA)2Cl4] XRD structure of the tetranuclear complex [Cu4(μ4-O)(LA)2Cl4] and view of the coordinative node µ4-O Cu4 | FTIR UV-vis Elemental analysis ESI-MS XRD |  | Indicator of achievement |  |
| 5. | XRD structure of the coordination network [Mn6(µ3-O)2(salox)6(H2salox)(H2O)3L] IR max (KBr), cm-1: 3388vs, 3053m, 2952m, 2925m, 2886m, 1707m, 1618s, 1600vs, 1536vs, 1498m, 1473s, 1442s, 1410s, 1358w, 1335m, 1313m, 1284s, 1264s, 1200m, 1152m, 1125m, 1043s, 1027vs, 958m, 919s, 896m, 838m, 787s, 748s, 677s, 648s, 560w, 531m, 472m, 401w. UV-Vis (DMF), max, nm (ε, dm3mol-1cm-1): 286 (87100), 380 (27474). Anal calc. for C68H75.4Mn6N8O27.2Si2 (Mr 1825. 78 g/mol): C 44.73.9, H 4.16, N 6.14; Found: C 45.02, H 4.42, N 6.32. The structure of the hexanulear cluster [Mn6(µ3-O)2(salox)6(H2salox)(H2O)3L] and view of the coordination polyhedra of the manganese atoms in hexanuclear cluster Mn6(µ3-O)2 TG/DTG and DSC curves of the coordination polymer [Mn6(µ3-O)2(salox)6(H2salox)(H2O)3L] | FTIR UV-vis Elemental analysis ESI-MS XRD TG/DTG DSC DVS AFM SEM TEM |  | Indicator of achievement |  |
|  | Sorption/desorption isotherms and AFM images of the coordination polymer [Mn6(µ3-O)2(salox)6(H2salox)(H2O)3L] TEM and SEM images of the coordination polymer [Mn6(µ3-O)2(salox)6(H2salox)(H2O)3L] from chloroform |  |  |  |  |
| 6. | {[Mn5L(cpdps)4(HCOO)2(H2O)2(DMF)4]·6DMF}n View of the pentanuclear cluster [Mn5] in the crystal structure of of the coordination network Connection of adjacent secondary building units [Mn5] by carboxylate ligands and view of the 3D structure of the coordination network | FTIR UV-vis Elemental analysis ESI-MS XRD TG/DTG DSC DVS |  | Indicator of achievement |  |
| 7. | {Mn3(μ-H2O)2(Hcpdps)2(cpdps)2(DMF)2]∙2DMF∙12H2O}n View of the trinuclear cluster in the crystal structure of the coordination network View of the 3D network in the crystal structure of the trinuclear complex TG/DTG curves of the pentanuclear and trinuclear coordination networks Sorption/desorption isotherms of the pentanuclear and trinuclear coordination networks | FTIR UV-vis Elemental analysis ESI-MS XRD TG/DTG DSC DVS |  | Indicator of achievement |  |
| Expected indicator: At least one presentation at scientific meeting; Achieved: 16 Presentations at International Scientific Meetings-2015 - Zaltariov, M., Cazacu, M., Shova, S., Structural diversity in Cu(II) and Co(II) complexes induced by flexible ligands, Seventh Cristofor I. Simionescu Symposium Frontiers in Macromolecular and Supramolecular Science 4-5 June, 2015, Iasi, Romania- oral presentation. - Iacob, M., Racles, C., Tugui, C., Stiubianu, G., Cazacu, M., μ3-oxotrinuclear iron carboxy-clusters as effective alternative sources for their oxide nanoparticles. 15th International Balkan Workshop on Applied Physics, Constanta, 2-4 June 2015- oral presentation. - Iacob, M., Stiubianu, G., Tugui, C., Bele, A., Cazacu. M., Managing silicone electromechanical properties through inorganic nanoparticles fillers. 14th World Renewable Energy Congress - WREC 2015, Bucuresti, Romania, 8-12 iunie- oral presentation. - Iacob, M., Silicon nanocomposites as dielectric elastomers. Modern Science and Energy, The XXXIII-rd Edition, Cluj, 14-15 May 2015 - oral presentation. - Iacob, M., Cazacu, M., Racles, C., Patras, X., Stiubianu, G., Tugui, C., Bele, A., Sacarescu, L., Turta, C. Preparation of magnetic nanoparticles for biomedical applications. International Congress “Preparing the future by promoting the excellence“, The XXV-th Edition, Section B– Landmarks in modern medicine. Apollonia University, Iasi, Romania 26 february – 1 march 2015- oral presentation. - Zaltariov, M., Vlad, A., Cazacu, M., Shova, S., Discrete structures and extended networks built by flexible ligands and Zn(II) ions, 19-th Romanian International Conference on Chemistry and Chemical Engineering September 2-5 , 2015, Sibiu, Romania- oral presentation. - Zaltariov, M., Cazacu, M., Vlad, A., Shova, S., Mn(II) and Zn(II)-organic frameworks: toward new magnetic and luminescent materials, The 3rd CEEPN Workshop on Polymer Science, September 23-26, 2015, Iasi, Romania- oral presentation. - Cazacu, M., Soroceanu, A., Zaltariov, M., Metal complexes with ligands containing dimethylsiloxane units: self-assembling ability, The XVIII-th International Conference "Physical Methods in Coordination and Supramolecular Chemistry" (dedicated to the memory of professor Constantin Turta and professor Mihail Revenco), October 8 – 9, 2015, Chişinău, Moldova- oral presentation - Dascalu, M., Balan, M., Shova,S., Racles, C., Cazacu, M., Ferrocenylsiloxane urea: synthesis, structure and properties, The XVIII-th International Conference "Physical Methods in Coordination and Supramolecular Chemistry" (dedicated to the memory of professor Constantin Turta and professor Mihail Revenco), October 8 – 9, 2015, Chişinău, Moldova- oral presentation - Vlad, A., Cazacu, M., Shova, S., Zaltariov, M., Self-Assembled Cu(II) Coordination Complexes Based on Mixed Ligands: Silicon-Containing Carboxylic Acids and N-Donor Ligand - 19-th Romanian International Conference on Chemistry and Chemical Engineering September 2-5 , 2015, Sibiu, Romania-poster. |  |  | Result indicator |  |
| - Vlad, A., Zaltariov, M., Cazacu, M., Shova, S., 2D manganese(II) networks based on V-shaped bis(p-carboxyphenyl)diphenylsilane: synthesis, structures and properties, The XVIII-th International Conference "Physical Methods in Coordination and Supramolecular Chemistry" (dedicated to the memory of professor Constantin Turta and professor Mihail Revenco), October 8 – 9, 2015, Chişinău, Moldova-poster. - Iacob, M., Tugui, C., Sirbu, D, Stiubianu, G., Cazacu, M., Superparamagnetic iron oxide nanowires self-assembled into smectic crystal. The XVIIIth International Conference "Physical Methods in Coordination and Supramolecular Chemistry". Chişinău, Moldova, 8-9 Octombrie 2015, poster. Presentations at National Scientific Meetings--2015 - Zaltariov, M., Cazacu, M., Shova, S., Vlad, A., Synthesis, structural characterization and magnetic properties of a polymerc complex built by hexanuclear clusters and flexible ligands, Iasi Academic Days-The XXV-th Session of scientific communications of „Petru Poni„ Institute of Macromolecular Chemistry Iasi, 24 - 26 september 2015- oral presentation - Soroceanu, A., Cazacu, M., Metallic complexes with Schiff base ligand containing siloxane segment, Iasi Academic Days-The XXV-th Session of scientific communications of „Petru Poni„ Institute of Macromolecular Chemistry Iasi, 24 - 26 september 2015- oral presentation - Vlad, A., Cazacu, M., Shova, S., Zaltariov, M., Metallic complexes of flexible Schiff bases self-assembled in supramolecular structures, Iasi Academic Days-The XXV-th Session of scientific communications of „Petru Poni„ Institute of Macromolecular Chemistry Iasi, 24 - 26 september 2015- poster - Zaltariov, M., Vlad, A., Cazacu, M., Shova, S., Cu(II) and Zn(II) complexes of Schiff bases derived from trimethylsilyl-propyl-p-aminobenzoate, Zaltariov, Iasi Academic Days-The XXV-th Session of scientific communications of „Petru Poni„ Institute of Macromolecular Chemistry Iasi, 24 - 26 september 2015- poster. |  |  |  |  |
| (Expected indicator: At least two scientific articles submitted at ISI journals; Achieved: 11 (articles published in ISI journals). Published articles: - Zaltariov, M. F., Cazacu, M., Vlad, A., Sacarescu, L., Shova, S., Coordination polymer of copper with a silicon-containing Schiff base: synthesis, structural characterization, properties, High Perform. Polym. 2015, 27(5), 607–615. - Zaltariov, M. F., Cazacu, M., Avadanei, M., Shova, S., Balan, M., Vornicu, N., Vlad, A., Dobrov, A., Varganici, C. D., Synthesis, characterization and antimicrobial activity of new Cu(II) and Zn(II) complexes with Schiff bases derived from trimethylsilyl-propyl-p-aminobenzoate, Polyhedron 2015, 100, 121–131. - Cazacu, M., Shova, S., Soroceanu, A., Machata, P., Bucinsky, L., Breza, M., Rapta, P., Telser, J., Krzystek, J., Arion, V. B., Charge and spin states in Schiff base metal complexes with a disiloxane unit exhibiting a strong noninnocent ligand character: synthesis, structure, spectroelectrochemistry, and theoretical calculations, Inorg. Chem., 2015, 54 (12), 5691–5706. - Soroceanu, A., Cazacu, M., Racles, C., Stoica, I., Săcărescu, L., Varganici, C. D., Supramolecular aggregation in organic solvents of discrete copper complexes formed with organosiloxane ligands, Soft Mater. 2015, 13, 93-105. - M. Iacob, D. Sirbu,C. Tugui, G. Stiubianu, L. Sacarescu, V. Cozan, A. Zeleňáková, E. Čižmár, A. Feher, M. Cazacu. Superparamagnetic amorphous iron oxide nanowires self-assembled into ordered layered structures. RSC Advances 2015, 5, 62563-62570 - M. Iacob, G. Stiubianu, C. Tugui, E.L. Ursu, M. Ignat, C. I. Turta, M. Cazacu. Goethite nanorods as cheap and effective filler for siloxane nanocomposite elastomers. RSC Advances 2015, 5, 45439-45446. - M. Iacob, M. Cazacu, C. Turta, F. Doroftei, M. Botko, E. Čižmár, A. Zeleňáková, A. Feher. Amorphous iron–chromium oxide nanoparticles with long-term stability. Materials Research Bulletin, 2015, 65, 163-168. - M. Iacob. Sonochemical synthesis of hematite nanoparticles. Chemistry Journal of Moldova, 2015, 1, 46-51. - Dumitriu, C., Cazacu, M., Bargan, A., Balan, M., Vornicu, N., Varganici, C. D., Shova, S., J. Organomet. Chem. 2015, 799-800, 195-200. - Dascalu, M., Musteata, V. E., Vacareanu, L., Racles, C., Cazacu, M., Synthesis and Characterization of Metal-Containing Poly(siloxane-urethane) Crosslinked Structures Derived from Siloxane Diols and Ferrocene Diisocyanate, RSC. Advances-2015, DOI: 10.1039/c5ra15290a. - Dascalu, M., Balan, M., Shova,S., Racles, C., Cazacu,M., Design and synthesis of the first ferrocenylsiloxane urea: structure and properties, Polyhedron-2015, doi:10.1016/j.poly.2015.11.013. |  |  | Result indicator |  |
| Scientific Report: - achieved indicator All the objectives of this stage of project – 2015 were achieved! |  |  | Result indicator |  |