THE 2nd CEEPN WORKSHOP ON

POLYMER SCIENCE

October 24-25, 2014, Iasi, Romania

“Petru Poni” Institute of Macromolecular Chemistry

41A Grigore Ghica Voda Alley, 700487 Iasi, Romania

Organized under the auspices of the bilateral Romanian-Ukrainian interacademic project “Development of multifunctional organic and organic-inorganic polymeric materials on the base of components with different chemical nature”, 2012-2016

Workshop Topic

POLYMER SCIENCE – a powerful tool for

highly specialized functional materials

International Scientific Committee:

Acad. Bogdan SIMIONESCU (Romania)

Acad. Eugene LEBEDEV (Ukraine)

Dr. Valeria HARABAGIU (Romania)

Prof. Yuri SAVELYEV (Ukraine)

Assoc. Prof. Neli KOSEVA (Bulgaria)

Dr. Frantisek RYPACEK (Czech Republic)

Prof. Bela IVAN (Hungary)

Prof. Andrzej DWORAK (Poland)

Prof. Marek KOWALCZUK (Poland)

Prof. Igor LACIK (Slovakia)

Dr. Ema Žagar (Slovenia)

Organizing committee:

Dr. Madalina ZANOAGA (Romania)

Dr. Yevgen MAMUNYA (Ukraine)

Dr. Fulga TANASA (Romania)

Dr. Maksym IURZHENKO (Ukraine)

Dr. Marioara NECHIFOR (Romania)

Dr. Viorica GAINA (Romania)

Dr. Volodymyr LEVCHENKO (Ukraine)

Mrs. Mioara SAVA (Romania)

Mrs. Sinziana VLAD (Romania)

|  | The organizers gratefully acknowledge the assistance of our partners. |  |
| --- | --- | --- |
| FP7-REGPOT-2010-1 Nr. 264115 |

We thank our sponsor for the financial support:

Societatea comercială S. C. LABORATORIUM S. R. L.

THE 2nd CEEPN WORKSHOP ON

POLYMER SCIENCE

October 24-25, 2014

POLYMER SCIENCE – a powerful tool for

highly specialized functional materials

PROGRAMME

Friday, October 24, 2014

Conference hall

| 8:00 - 8:30 | Participants registration |
| --- | --- |
| SESSION 1 – Moderators: Dr. Valeria Harabagiu (PPIMC, Iasi, Romania) Dr. Ivan Chodák (PISAS, Bratislava, Slovakia) |
| 8:30 - 8:40 | Opening speech | Acad. Bogdan C. Simionescu (PPIMC, Iasi, Romania) |
| 8:40 - 9:20 | Plenary lecture (L1) | Igor Lacik (PISAS, Bratislava, Slovakia) |
| 9:20 - 10:00 | Plenary lecture (L2) | Yevgen P. Mamunya (IMC, Kiev, Ukraine) |
| 10:00 - 10:15 | Oral communication (Co1) | Malgorzata Basko (CMMS, Lodz, Poland) |
| 10:15 - 10:30 | Oral communication (Co2) | Daniel G. Angelescu (IMIPC, Bucharest, Romania) |
| 10:30 - 10:45 | Oral communication (Co3) | Viorica Elena Podasca (PPIMC, Iasi, Romania) |
| 10:45 - 11:15 | Coffee break |
| SESSION 2 – Moderators: Dr. Sergiu Coseri (PPIMC, Iasi, Romania) Dr. Bozena Jarzabek (CPCM, Zabrze, Poland) |
| 11:15 - 11:55 | Plenary lecture (L3) | Hynek Beneš (IMC, Prague, Czech Republic) |
| 11:55 - 12:35 | Plenary lecture (L4) | Neli S. Koseva (IPBAS, Sofia, Bulgaria) |
| 12:35 - 12:50 | Oral communication (Co4) | Magdalena Wójtowicz (CPCM, Zabrze, Poland) |
| 12:50 - 13:05 | Oral communication (Co5) | Denys Chervakov (SHEI, Dnipropetrovsk, Ukraine) |
| 13:05 - 14:00 14:00 - 15:00 | Lunch Visit at PPIMC, Iasi, Romania |
| SESSION 3 – Moderators: Dr. Mariana Pinteala (PPIMC, Iasi, Romania) Dr. Hynek Beneš (IMC, Prague, Czech Republic) |
| 15:00 - 15:40 | Plenary lecture (L5) | Ivan Chodák (PISAS, Bratislava, Slovakia) |
| 15:40 - 16:20 | Plenary lecture (L6) | Bozena Jarzabek (CPCM, Zabrze, Poland) |
| 16:20 - 16:35 | Oral communication (Co6) | Ioana M. Simionca (PPIMC, Iasi, Romania) |
| 16:35 - 16:50 | Oral communication (Co7) | Piotr Kubica (CPCM, Zabrze, Poland) |
| 16:50 - 17:20 | Coffee break |
| SESSION 4 – Moderators: Dr. Malgorzata Basko (CMMS, Lodz, Poland) Dr. Daniel Timpu (PPIMC, Iasi, Romania) |
| 17:20 - 18:00 | Plenary lecture (L7) | Mariana Cristea (PPIMC, Iasi, Romania) |
| 18:00 - 18:15 | Oral communication (Co8) | Daniela Ionita (PPIMC, Iasi, Romania) |
| 18:15 - 18:30 | Oral communication (Co9) | Cristina-Eliza Brunchi (PPIMC, Iasi, Romania) |
| POSTERS – permanent session Moderators: Dr. Madalina Zanoaga (PPIMC, Iasi, Romania) Dr. Volodymyr Levchenko (IMC, Kiev, Ukraine) Dr. Raluca Darie (PPIMC, Iasi, Romania) Dr. Piotr Kubica (CPCM, Zabrze, Poland) |

Saturday, October 25, 2014

Conference hall

| SESSION 5 – Moderators: Dr. Maria Bruma (PPIMC, Iasi, Romania) Dr. Hynek Beneš (IMC, Prague, Czech Republic) |
| --- |
| 8:30 - 9:10 | Plenary lecture (L8) | Kristina G. Gusakova (IMC, Kiev, Ukraine) |
| 9:10 - 9:50 | Plenary lecture (L9) | Valentin I. Popa (GATU, Iasi, Romania) |
| 9:50 - 10:30 | Plenary lecture (L10) | Marian Valentin (PISAS, Bratislava, Slovakia) |
| 10:30 - 10:45 | Oral communication (Co10) | Camelia Hulubei (PPIMC, Iasi, Romania) |
| 10:45 - 11:00 | Oral communication (Co11) | Vasile Cristian Grigoras (PPIMC, Iasi, Romania) |
| 11:00 - 11:15 | Oral communication (Co12) | Ada Ionela Burescu (PPIMC, Iasi, Romania) |
| 11:15 - 11:45 | Coffee break |
| SESSION 6 – Moderators: Dr. Daniela Ivanov (PPIMC, Iasi, Romania) Dr. Marian Valentin (PISAS, Bratislava, Slovakia) |
| 11:45 - 12:25 | Plenary lecture (L11) | Marcela Mihai (PPIMC, Iasi, Romania) |
| 12:25 - 13:05 | Plenary lecture (L12) | Maksym V. Iurzhenko EOPEWI and IMC, Kiev, Ukraine |
| 13:05 - 13:20 | Oral communication (Co13) | Mirela Teodorescu (PPIMC, Iasi, Romania) |
| 13:20 - 13:35 | Oral communication (Co14) | Anca Grigoras (PPIMC, Iasi, Romania) |
| 13:35 - 13:50 | Oral communication (Co15) | Volodymyr Levchenko (IMC, Kiev, Ukraine) |
| 13:50 - 14:50 14:50 - 16:00 | Lunch Visit at Intelcenter, PPIMC, Iasi, Romania |
| 16:00 | Discussion. Concluding remarks and workshop closure. The CEEPN meeting. |

ACRONYMS

| CEEPN | Central and Est European Polymer Network |
| --- | --- |
| CMMS | Center of Molecular and Macromolecular Studies, Lodz, Poland |
| CPCM | Centre of Polymer and Carbon Materials, Polish Academy of Sciences, Zabrze, Poland |
| EOPEWI | E.O.Paton Electric Welding Institute, National Academy of Sciences of Ukraine, Kiev, Ukraine |
| GATU | “Gheorghe Asachi” Technical University, Iasi, Romania |
| IMC | Institute of Macromolecular Chemistry, Kiev, Ukraine |
| IMIPC | “Ilie Murgulescu” Institute of Physical Chemistry, Bucharest, Romania |
| IPBAS | Institute of Polymers, Bulgarian Academy of Sciences, Sofia, Bulgaria |
| PISAS | Polymer Institute of the Slovak Academy of Sciences, Bratislava, Slovakia |
| PPIMC | “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| SHEI | State High Educational Institute “Ukrainian State University of Chemical Technology”, Dnipropetrovsk , Ukraine |

Friday, October 24, 2014

Conference hall

| 8:00-8:30 | Participants registration |
| --- | --- |
| 8:30-8:40 | Workshop opening - Acad. Bogdan C. Simionescu (PPIMC) |

| SESSION 1 – Moderators: Dr. Valeria Harabagiu (PPIMC, Iasi, Romania) Dr. Ivan Chodák (PISAS, Bratislava, Slovakia) |
| --- |
| 8:40 - 9:20 | L1 | POLYZWITTERIONS: PROPAGATION KINETICS, HYDROGELS, NON-BIOFOULING COATINGS P. Kasak1,2, P. Sobolciak1,2, V. Semak1, M. Stach1, Z. Kronekova1, G. Hlouskova1, I. Krupa1,2, D. Chorvat3, P. Rychter1, L. Uhelska1, I. Lacik1 1 Polymer Institute SAS, Department for Biomaterials Research, Bratislava, Slovakia 2 Current address: Center for Advanced Materials, Qatar University, Doha, Qatar 3 International Laser Centre, Department of Biophotonics, Bratislava, Slovakia |
| 9:20 - 10:00 | L2 | Polymer composites – interrelations between structure and electrical and thermal properties Ye. P. Mamunya Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| 10:30 - 10:45 | Co1 | CATIONIC COPOLYMERIZATION OF RACEMIC-β-BUTYROLACTONE WITH L,L-LACTIDE M. Basko1, A. Duda1, S. Kazmierski2, P. Kubisa1 Center of Molecular and Macromolecular Studies, Lodz, Poland 1 Department of Polymer Chemistry 2 Laboratory for Analysis of Organic Compounds and Polymers |
| 10:15 - 10:30 | Co2 | CONFORMATIONAL PROPERTIES OF MULTIGRAFT HOMOPOLYMERS IN GOOD SOLVENT. A COMPUTER SIMULATION INVESTIGATION D. G. Angelescu1, G. Munteanu1, P. Linse2 1 Romanian Academy, “Ilie Murgulescu” Institute of Physical Chemistry, Bucharest, Romania 2 Physical Chemistry, Lund University, Lund, Sweden |
| 10:00 - 10:15 | Co3 | PHOTOPOLYMERIZABLE COMPOSITES BASED ON VINYL ACETATE, p-ACRYLOYLOXYBENZALDEHYDE AND N-METHACRYLOYLOXYETHYL-N’-FLUORESCEINYL UREA AS ORGANIC MATRICES FOR SILVER NANOPARTICLES V. E. Podasca, T. Buruiana, E. C. Buruiana “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 11:30-12:00 | Coffee break |
| SESSION 2 – Moderators: Dr. Bozena Jarzabek (CPCM, Zabrze, Poland) Dr. Sergiu Coseri (PPIMC, Iasi, Romania) |
| 11:15 - 11:55 | L3 | MICROWAVE-ASSISTED DEGRADATION OF PLASTICS H. Beneš, A. Gawełczyk, P. Horák, D. Rais, Z. Kruliš Institute of Macromolecular Chemistry, Academy of Sciences of the Czech Republic, Prague, Czech Republic |
| 11:55 - 12:35 | L4 | Polyphosphoester based delivery systems of anticancer agents N. S. Koseva, V. A. Mitova, A. Bogomilova, K. D. Troev Institute of Polymers, Bulgarian Academy of Sciences, Sofia, Bulgaria |
| 12:35 - 12:50 | Co4 | GAS AND VAPOR TRANSPORT PROPERTIES OF AROMATIC AND SEGMENTED POLYIMIDES M. Wójtowicz, E. Grabiec, A. Jankowski, A. Wolińska-Grabczyk Centre of Polymer and Carbon Materials, Polish Academy of Sciences, Zabrze, Poland |
| 12:50 - 13:05 | Co5 | GLASS FIBER COMPOSITES BASED ON USED POLYETHYLENE TEREPHTHALATE D. Chervakov, O. Chervakov State High Educational Institute «Ukrainian State University of Chemical Technology», Dnipropetrovsk, Ukraine |
| 13:05-14:00 | Lunch |
| 14:00-15:00 | Visit at PPIMC, Iasi, Romania |
| SESSION 3 – Moderators: Dr. Mariana Pinteala (PPIMC, Iasi, Romania) Dr. Hynek Beneš (IMC, Prague, Czech Republic) |
| 15:00 - 15:40 | L5 | Structure of reinforcing filler network determined by electrical conductivity of the polymer / carbon black composite I. Chodák, J. Krajči Polymer Institute of the Slovak Academy of Sciences, Bratislava, Slovakia |
| 15:40 - 16:20 | L6 | UV-VIS-NIR(T) SPECTROSCOPY, AS A METHOD TO INVESTIGATE THERMAL STABILITY OF POLYMER THIN FILMS B. Jarzabek Center of Polymer and Carbon Materials Polish Academy of Sciences, Zabrze, Poland |
| 16:20 - 16:35 | Co6 | RAFT-MEDIATED COPOLYMERIZATION OF N-(2-HYDROXYPROPYL)METHACRYLAMIDE WITH N-ACRYLOXYSUCCINIMIDE AND SUBSEQUENT MODIFICATION OF THE COPOLYMER I. M. Simionca1, J. Moraes2, H. Ketari2, H. A. Klok2, M. Pinteala1 1 Centre of Advanced Research in Bionanoconjugates and Biopolymers, “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 École Polytechnique Fédérale de Lausanne (EPFL), Institut des Matériaux and Institut des Sciences et Ingénierie Chimiques, Laboratoire des Polymères, Bâtiment MXD, Lausanne, Switzerland |
| 16:35 - 16:50 | Co7 | HYBRID MEMBRANES COMPOSED OF POLYSULFONE MATRIX AND ZEOLITE OR METAL-ORGANIC FRAMEWORK PARTICLES P. Kubica, A. Jankowski, A. Wolinska-Grabczyk Centre of Polymer and Carbon Materials, Polish Academy of Sciences, Zabrze, Poland |
| 16:50 - 17:20 | Coffee break |
| SESSION 4 – Moderators: Dr. Malgorzata Basko (CMMS, Lodz, Poland) Dr. Daniel Timpu (PPIMC, Iasi, Romania) |
| 17:20 - 18:00 | L7 | PLGA-BASED NON-WOWEN FABRICS. CHALLENGES IN THE INTERPRETATION OF THE DYNAMIC MECHANICAL ANALYSIS RESULTS M. Cristea1,5, W. Sikorska2,5, P. Dobrzynski2,5, D. Ionita1,5, G. Adamus2,5, I. Krucinska3, A. Komisarczyk3, M. Kowalczuk2,4,5 1,5 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2,5 Polish Academy of Sciences, Centre of Polymer and Carbon Materials, Zabrze, Poland 3 Department of Material and Commodity Sciences and Textile Metrology, Lodz University of Technology, Lodz, Poland 4 School of Biology, Chemistry and Forensic Science, Faculty of Science and Engineering, University of Wolverhampton, Wolverhampton, UK 5 Central and East European Polymer Network, ADVAPOL Laboratory |
| 18:00 - 18:15 | Co8 | THERMAL AND MECHANICAL RESPONSE IN POLYURETHANES BASED ON DBDI D. Ionita1,2, M. Cristea1, C. Gaina1, D. Banabic2 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 Technical University of Cluj-Napoca, Cluj-Napoca, Romania |
| 18:15 - 18:30 | Co9 | THERMODYNAMIC ASPECTS CONCERNING THE XANTHAN BEHAVIOR IN DILUTE SOLUTION C.-E. Brunchi, S. Morariu, M. Bercea “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| POSTERS – permanent session Moderators: Dr. Madalina Zanoaga (PPIMC, Iasi, Romania) Dr. Volodymyr Levchenko (IMC, Kiev, Ukraine) Dr. Raluca Darie (PPIMC, Iasi, Romania) Dr. Piotr Kubica (CPCM, Zabrze, Poland) |

Saturday, October 25, 2014

Conference hall

| SESSION 5 – Moderators: Dr. Maria Bruma (PPIMC, Iasi, Romania) Dr. Hynek Beneš (IMC, Prague, Czech Republic) |
| --- |
| 8:30 - 9:10 | L8 | Effect of processing conditions on viscoelastic and thermal characteristics of Cyanate Ester Resin/organoClay nanocomposites K. G. Gusakova1, A. M. Fainleib1, O. P. Grigoryeva1, J. M. Saiter2, N. S. Lavrenyuk1 1 Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine 2 AMME-LECAP International Lab. Institute for Material Research, Université de Rouen, Faculté des sciences, Saint Etienne du Rouvray, France |
| 9:10 - 9:50 | L9 | FREE RADICAL REACTIONS IN BIOLOGICAL SYSTEMS –A CONCEPT APPROACHED IN THE RESEARCHES CARRIED OUT BY PROFESSOR CRISTOFOR I. SIMIONESCU V. I. Popa (Gh. Asachi( Technical University, Faculty of Chemical Engineering and Environmental Protection, Iasi, Romania |
| 9:50 - 10:30 | L10 | NANOINDENTATION AND ITS APPLICATION FOR THE STUDY OF PLASMA TREATED POLY(LACTIC ACID) SURFACE M. Valentin1, A. Skarmoutsou2, I. Novák1, I. Krupa1, M. Omastová1 1 Polymer Institute, Slovak Academy of Science, Bratislava, Slovakia 2School of Chemical Engineering, National Technical University of Athens, Athens, Greece |
| 10:30 - 10:45 | Co10 | NEW MATERIALS BASED ON POLYIMIDES CONTAINING ALICYCLIC UNITS C. Hulubei, D. Popovici, C. D. Vlad, I. Stoica, M. Bruma, S. Ioan “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 10:45 - 11:00 | Co11 | CRYSTALLIZATION DYNAMICS IN COPOLYAMIDE-CLAY HYBRID NANOCOMPOSITES V. C. Grigoras, M. Zanoaga, F. Tanasa “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 11:00 - 11:15 | Co12 | COMPARED PROPERTIES OF THIN FILMS MADE FROM AZO-POLYIMIDES A. I. Burescu1, I. Sava1, I. Stoica1, V. Musteata1, I. Topala2, M. Bruma1 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 “Alexandru Ioan Cuza” University of Iasi, Faculty of Physics, Plasma Advanced Research Center (IPARC), Iasi, Romania |
| 11:15 - 11:45 | Coffee break |
| SESSION 6 – Moderators: Dr. Daniela Ivanov (PPIMC, Iasi, Romania) Dr. Marian Valentin (PISAS, Bratislava, Slovakia) |
| 11:45 - 12:25 | L11 | POLYELECTROLYTES IN CALCIUM CARBONATE MINERALIZATION M. Mihai “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 12:25 - 13:05 | L12 | WELDING OF PLASTICS: FROM BASIC APPROACHES TO FUNDAMENTAL KNOWLEDGE M. V. Iurzhenko1,2 1 E. O. Paton Electric Welding Institute, National Academy of Sciences of Ukraine, Kiev, MSP, Ukraine 2 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| 13:05 - 13:20 | Co13 | PHYSICAL HYDROGELS OF POLY(VINYL ALCOHOL) /POLY(VINYLPYRROLIDONE) M. Teodorescu, M. Bercea, S. Morariu “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 13:20 - 13:35 | Co14 | NEW PULLULAN DERIVATIVES. LASER LIGHT SCATTERING AND TURBIDITY STUDIES A. G. Grigoras, M. Constantin Fundueanu “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| 13:35 - 13:50 | Co15 | VOLUME-STRUCTURED POLYMERIC MATERIALS WITH GIANT PERMITTIVITY V. Levchenko1, G. Boiteux2, E. Beyou2, P. Alcouffe2, G. Seytre2, Ye. Mamunya1, A. Serghei2 1 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Université Lyon 1, CNRS-UMR 5223, Ingénierie des Matériaux Polymères, IMP@Lyon1, France |
| 13:50 - 14:50 | Lunch |
| 14:50 - 16:00 | Visit at IntelCentru, PPIMC, Iasi, Romania |
| 16:00 - 18:00 | Horizon 2020 – opportunities for joint projects |
| 18:00 | Discussion. Concluding remarks and workshop closure The CEEPN meeting |

POSTERS – permanent session

Friday, October 24- Saturday, October25, 2014

Conference hall

| P1 | VISCOELASTIC PROPERTIES OF INTERPENETRATING POLYMER NETWORKS BASED ON POLYURETHANE AND ORGANIC-INORGANIC COPOLYMER N. V. Babkina, I. S. Martynyuk, T. T. Alekseeva Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| --- | --- |
| P2 | NONISOCYANATE EPOXYPOLYURETHANES FOR POLYMERIC COMPOSITE MATERIALS A. V. Barantsova, A. Y. Filipovych, V. K. Grishchenko, L. V. Ermolchuk Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P3 | CORROSION RESISTANT POLYMERIC MATERIALS BASED ON OLIGODIENES WITH TERMINAL FUNCTIONAL GROUPS A. V. Barantsova, V. K. Grishchenko, N. A. Busko, N. V. Gudzenko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P4 | EFFECT OF SALT AND HEAT TREATMENT ON AQUEOUS XANTHAN SOLUTIONS C.-E. Brunchi “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P5 | POLYIONENS BASED ON TETRAHYDRO-1,4-OKSAZYN AND EPOXIDIZED DERIVATIVES OF 1,2-EPOXY-4,7-8-DIOKSONONEN M. V. Burmistr, O. S. Sverdlikovska, O. O. Fedenko State High Educational Institute «Ukrainian State University of Chemical Technology», Dnipropetrovsk, Ukraine |
| P6 | SYNTHESIS AND PROPERTIES OF BLOCK COPOLYMERS PREPARED FROM OLIGOMERIC POLYAZOINITIATORS OF VEGETABLE OILS N. A. Busko, V. K. Grishchenko, A. V. Barantsova, Ya. V. Babkina, N. V. Kochetova, U. A. Silchenko, S. N. Ostapyuk, N. V. Gudzenko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P7 | TECHNOLOGIES FOR THE FATTY ACID ESTERS SYNTHESIS USING POLYMERIC HETEROGENEOUS CATALYSTS O. V. Chervakov, K. O. Gerasymenko, T. G. Filinska State High Educational Institute “Ukrainian State University of Chemical Technology”, Dnipropetrovsk, Ukraine |
| P8 | THERMAL PROTECTION MATERIALS OF SPECIAL APPLICATION O. V. Chervakov1, Yu. A. Suvorova1, A. I. Matsuka1, D. O. Chervakov1, A. N. Simbirkina2, A. M. Potapov2 1 State High Educational Institute “Ukrainian State University of Chemical Technology”, Dnipropetrovsk, Ukraine 2 Yuzhnoye State Design Office, Dnepropetrovsk, Ukraine |
| P9 | THIOPHENE-FUNCTIONALIZED BIOCOMPATIBLE/ BIODEGRADABLE MACROMONOMERS: RING OPENING POLYMERIZATION (ROP) AT WORK IN THE BENEFIT OF “HAIRY-ROD” CONJUGATED POLYMERS A.–D. Bendrea, L. Cianga, I. Cianga “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P10 | AMPHIPHILIC POLY(p-PHENYLENE VINYLENE) “HAIRY-RODS”: SYNTHESIS, CHARACTERIZATION AND SELF-ASSEMBLY IN WATER I. Cianga1, D. Göen Çolak2, L. Cianga1, A.-D. Bendrea1, Y. Yagci2,3 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 Department of Chemistry, Faculty of Science and Letters, Istanbul Technical University, Istanbul, Turkey 3 Department of Chemistry, King Abdulaziz University, Jedahh, Saudi Arabia |
| P11 | TOWARD “GREEN”, FLEXIBLE COTTON-BASED COMPOSITE MATERIALS OBTAINED BY “IN SITU” STEP-GROWTH POLYMERIZATION OF DIFFERENT THIOPHENE MONOMERS VIA PHOTOINDUCED ELECTRON TRANSFER REACTIONS L. Cianga1,2, F. Tanasa1, C. M. Loghin3, I. Cianga1,2, D.G. Colak2, S. Timur4, Y. Yagci2,5 1”Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 Department of Chemistry, Faculty of Science and Letters, Istanbul Technical University, Istanbul, Turkey 3 Faculty of Textile and Leather Engineering, “Gheorghe Asachi” Technical Univeristy, Iasi, Romania 4 Department of Biochemistry, Faculty of Science, Ege University, Izmir, Turkey 5 Center of Excellence for Advanced Materials Research (CEAMR), Department of Chemistry, Faculty of Science, King Abdulaziz University, Jeddah, Saudi Arabia |
| P12 | BLOCKED ISOCYANATES AS POLYSACCHARIDES MODIFIERS K. S. Didenko, N. V. Kozak, V. V. Klepko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P13 | PYROLYTIC MASS-SPECTROMETRY OF SOME LIQUID RUBBERS OBTAINED BY RADICAL POLYMERIZATION Т. V. Dmitrieva, V. I. Bortnitsky, V. P. Boiko, V. K. Grishchenko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P14 | CERAMIC FIBERS OF NiO, ZnO AND NiO-ZnO BASED ON AN ELECTROSPUN PSU/NICKEL AND ZINC ACETATE PRECURSOR P. (Dorneanu) Pascariu1,2, A. Airinei1, N. Olaru1, V. Nica2 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 Faculty of Physics, “Al. I. Cuza” University, Iasi, Romania |
| P15 | COMPLEX MACROMOLECULAR TEMPLATES FOR CALCIUM CARBONATE MICROPARTICLES GROWTH F. Doroftei, M. Mihai, B. C. Simionescu “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P16 | Effect of multiwalled carbon nanotubes on crystallinity of in situ polymerized oligomeric cyclic butylene terephthalate A. Fainleib1, O. Grigoryeva1, L. Bardash1, G. Boiteux2 1 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Université de Lyon, Lyon, F-69003, France; Université Lyon 1, IMP/LMPB Laboratoire des Matériaux Polymères et Biomatériaux, Bât ISTIL, Villeurbanne, France; CNRS, UMR5223, Ingénierie des Matériaux Polymères, Villeurbanne, France |
| P17 | PLASTICIZERS BASED ON RENEWABLE RAW MATERIALS FOR MIXED POLYMER COMPOSITES V. A. Fedoruk, K. Y. Varlan, E. A. Sporyagin Department of Chemistry and Chemical Technology of High Molecular Weight Compounds, Oles Honchar Dnepropetrovsk National University, Dnepropetrovsk, Ukraine |
| P18 | HYBRID MATERIALS BASED ON (ALLYL-BENZOXAZINE)S C. Gaina1, V. Gaina1, A. Chebac1, M. Iurzhenko2 1 “Petru Poni” Institute of Macromolecular Chemistry, Ias, Romania 2 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P19 | SPECIFIC LAYER-BY-LAYER BUTT WELDING OF MULTI-LAYER POLYMERIC COMPOSITE PIPES BASED ON POLYPROPYLENE AND GLASS FIBERS A. M. Galchun1, M. G. Korab1, V. Yu. Kondratenko1, A. O. Shadrin1, V. V. Anistratenko1, M. V. Iurzhenko1,2 1 E. O. Paton Electric Welding Institute, National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P20 | NEW NANOCOMPOSITES BASED ON POLYURETHANEACRYLATES WITH MODIFIED MONTMORILLONITE, PREPARED BY in situ POLYMERIZATION N. Gonchar, Yu. V. Savelyev, T.V. Travinskaya Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P21 | STRUCTYRE AND OPTICAL PROPERTIES OF THE COMPOSITES POLYVINILBUTYRAL/ZnO OBTAINED VIA SOL-GEL APPROACH E. V. Gres Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P22 | PREPARATION AND OPTICAL PROPERTIES OF HIGHLY HYDROPHILIC POLYMER STABILIZED ZnO NANOHYBRIDS E. V. Gres, A. L. Tolstov, E. V. Lebedev Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P23 | PHISICO-CHEMICAL AND MICROBIOLOGICAL EVALUATION OF TWO POLY(CARBOXYBETAINES) DERIVED FROM POLY(4-VINYLPYRIDINE) A. G. Grigoras, S. Racovita, S. Vasiliu, V. C. Grigoras “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P24 | INNOVATING FOOTWEAR DESIGN BASED ON BIOMECHANICAL AND PHYSIOLOGICAL PARAMETERS (INTERNATIONAL PROJECT) E. Grzesiak1, B. Woźniak1, Z. Olejniczak1, M. Broeckx2, I. Pospiech3 1 Leather Research Institute in Lodz, Poland 2 Thomas Moore University (MOBILAB), Belgium 3 Polish Chamber of Leather Industry, Poland |
| P25 | Electrical and electromechanical properties of some nanocomposite polyimide films C. Hamciuc1, E. Hamciuc1, M. Olariu2, M. Ignat3, L. Okrasa4, L. Dimitrov5, Y. Kalvachev5 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 “Gh. Asachi” Technical University, Electrical Engineering Faculty, Iasi, Romania 3 National Institute for Research and Development in Electrical Engineering ICPE-CA, Bucharest, Romania 4 Department of Molecular Physics, Lodz University of Technology, Lodz, Poland 5 Institute of Mineralogy and Crystallography, Sofia, Bulgaria |
| P26 | OPTICAL CHARACATERISTICS OF SOME FLUORINATED POLY(OXADIAXOLE ETHER)S IN NEAT AND MIXED SOLVENTS M. Homocianu, A. Airinei, C. Hamciuc, A. M. Ipate “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P27 | ELECTROPHYSICAL PROPERTIES AND RELAXATION BEHAVIOUR VERSUS STRUCTURAL ORGANIZATION OF THE ELECTROACTIVE HYBRID POLYMERS CONTAINING IONIC LIQUIDS M. Iurzhenko1,2 1 Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Center of Collective Use of Scientific Equipment for Thermophysical Investigations & Analysis of National Academy of Sciences of Ukraine in the Institute of Macromolecular Chemistry of NAS of Ukraine, Kiev, Ukraine |
| P28 | OPTICAL PROPERTIES OF THIN FILMS OF POLYAZOMETHINE WITH FLEXIBLE SIDE CHAINS B. Jarzabek, J. Weszka, B. Hajduk, J. Jurusik, M. Domanski Center of Polymer and Carbon Materials Polish Academy of Sciences, Zabrze, Poland |
| P29 | AMPHIPHILIC INVERTIBLE POLYMERS: SYNTHESIS, SELF-ASSEMBLY, AND APPLICATION A. M. Kohut1, A. S. Voronov2, S. A. Voronov1 1 Lviv Polytechnic National University, Department of Organic Chemistry, Lviv, Ukraine 2 North Dakota State University, Department of Coatings and Polymeric Materials, Fargo, USA |
| P30 | NITROXY PROBE DYNAMICS IN ORGANIC-INORGANIC COMPOSITES BASED ON POLYIMIDE DIFFERENT CHEMICAL STRUCTURE N. V. Kozak, T. A. Shantalii Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P31 | RESEARCH ON COMMERCIAL SBS RUBBERS, WITH DIFFERENT CONTENT OF CARBON BLACK, MODIFIED BY COLD PLASMA I. Krawczyk-Kłys1, P. Makowski2, I. Jaruga1, J. Tyczkowski2 1 Leather Research Institute, Lodz, Poland 2 Department of Molecular Engineering, Faculty of Process and Environmental Engineering, Technical University of Lodz, Lodz, Poland |
| P32 | MODIFIED POLY(VINYL CHLORIDE) PLASTICATES AND COMPOSITES BASED ON THEM Yu. V. Laruk, V. Ye. Levytskyj Lviv Polytechnic National University, Department of Polymer Processing, Lviv, Ukraine |
| P33 | ORGANIC-INORGANIC NANOSTRUCTURED POLYMER BLENDS N. N. Laskovenko, V. N. Lemeshko, E. V. Lebedev Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P34 | RELAXATION PROPERTIES OF CROSS-LINKED POLYURETHANES, MODIFIED WITH CARBONE NANOTUBES AND METAL COMPLEXES Eu. V. Lobko, Z. O. Gagolkina, Yu. V. Yakovlev, V. V. Klepko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P35 | PRELIMINARY STUDIES AND PROPERTIES EPOXY POLYURETANE COMPOSITE MATERIAL FILLED WITH POLYHYDROXYBUTYRATE AND DOXORUBICIN S. A. Lukashevich, R. A. Rozhnova, N. A. Galatenko, G. A. Kozlova, O. D. Shirokov Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P36 | PERCOLATION BEHAVIOR IN POLYETHYLENE GLYCOL-CARBON NANOTUBES SYSTEM E. A. Lysenkov1, V. V. Klepko2 1 Mykolayiv National University named after V.O. Sukhomlynskiy, Mykolayiv, Ukraine 2 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P37 | BIOACTIVE FOLATE-FERROCENE CONJUGATE L. V. Makeieva, R. A. Rozhnova, N. A. Galatenko, I. I. Gladyr Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P38 | ANISOTROPY OF PHYSICAL AND MECHANICAL PROPERTIES OF EPOXY SYSTEMS FORMED IN A MAGNETIC FIELD P. M. Malezhyk, T. G. Sichkar, N.M. Zazymko, N.I. Shut M. P. Dragomanov National Pedagogical University, Kiev, Ukraine |
| P39 | NANOSTRUCTURED POLYURETHANE ELASTOMER – POLY(VINIL CHLORIDE) BLENDS T. Malysheva Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P40 | AN INFLUENCE OF SODIUM SILICATE MODIFIED BY POLYACRYLIC ACID ON THE PROPERTIES OF ORGANIC-INORGANIC COMPOSITES T. Malysheva, Ye. Lebedev Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P41 | METHODS OF OBTAINING AND PROPERTIES OF FUNCTIONAL POLYMER-SILICATE COMPOSITES A. S. Masyuk, V. E. Levytskyj Lviv Polytechnic National University, Department of Chemical Technology of Plactics, Lviv, Ukraine |
| P42 | SOLID ION-CONDUCTIVE ELECTROLYTE BASED ON EPOXY OLIGOMER AND LiClO4 AT ELEVATED TEMPERATURE L. K. Matkovska1, M. V. Iurzhenko1, Ye. P. Mamunya1, O. K. Matkovska1, E. V. Lebedev1, G. Boiteux2, A. Serghei2 1 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Université de Lyon, Université Lyon 1, Ingénierie des Matériaux Polymères, UMR CNRS 5223, IMP@LYON1, France |
| P43 | EPOXYPHOSPHOTUNGSTIC POLYMER: STRUCTURE FORMATION O. K. Matkovska1, Ye. P. Mamunya1, G. Boiteux2, M. I. Shandruk1, O. V. Zinchenko1, E. V. Lebedev1 1 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Université Lyon 1, Ingénierie des Matériaux Polymères, UMR CNRS 5223, Villeurbanne, France |
| P44 | FACILE SYNTHESIS OF TITANOSILICATE COMPOSITES FOR CATALYTIC EPOXIDATION OF ALKENES V. F. Matyushov, E. V. Lebedev, A. L. Tolstov Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P45 | STAR-SHAPE POLYLACTIDE STEREOCOMPLEXES AS POTENTIAL MATERIALS TO DRUG DELIVERY SYSTEMS A. Michalski, A. Lewandowska, M. Brzezinski, T. Biela, A. Duda Department of Polymer Chemistry, Centre of Molecular and Macromolecular Studies, Polish Academy of Sciences, Lodz, Poland |
| P46 | PHOTOPHYSICAL PROPERTIES OF A SERIES OF OLIGOMERS WITH VINYLENE, IMINE, AZINE AND ETHYNYLENE SPACERS BEARING TRIPHENYLAMINE MOIETY B. Minaev1, E. Stromylo1, M. Grigoras2, L. Vacareanu2 1 Bogdan Khmelnitsky National University, Organic Chemistry Department, Cherkasy, Ukraine 2 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P47 | ELECTRICAL AND THERMAL CONDUCTIVITY OF EPOXY COMPOSITES CONTAINING METALLIC FILLERS A. I. Misiura1, Ye. P. Mamunya2 1 Taras Shevchenko National University of Kiev, Kiev, Ukraine 2 Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P48 | PREPARATION AND OPTICAL PROPERTIES OF POLYACRYLATES WITH LEUCINE AND PYRIDINE MOIETIES M. Murariu, E. C. Buruiana Petru Poni Institute of Macromolecular Chemistry, Iasi, Romania |
| P49 | Graft copolymer based on reactive olygomers of linseed oil and ethylene-vinyl acetate copolymer as a compatibilizer of composite polymer materials V. D. Myshak, О. М. Siryk, V. K. Grishchenko, E. V. Lebedev Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P50 | LIGHT-RESPONSIVE CHIRAL PHOTOCHROMIC POLYMER SYSTEMS O. Nadtoka, V. Syromyatnikov Taras Shevchenko National University of Kiev, Kiev, Ukraine |
| P51 | NEW 4-SUBSTITUTED 1,3-BIS(4-((E)-(PHENYLIMINO)METHYL)PHENOXY PROPAN-2-OLS WITH THE POTENTIAL NON-LINEAR OPTICAL PROPERTIES V. M. Ovdenko, A. Yu. Kolendo National Taras Shevchenko University of Kiev, Kiev, Ukraine |
| P52 | IMPROVE THE ANTIMICROBIAL ACTIVITY OF PARTIALLY CYCLOALIPHATIC CO-POLYIMIDE FILMS BY PLASMA TREATMENT D. Popovici1,2, C. Hulubei2, A. I. Barzic2, S. Ioan2, D. S. Vasilescu1, S. Dunca3 1 University ”POLITEHNICA” of Bucharest, Faculty of Applied Chemistry and Materials Science, Bucharest, Romania 2 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 3 “Al. I. Cuza” University of Iasi, Faculty of Biology, Iasi, Romania |
| P53 | INFLUENCE OF THE MICROBIAL CULTURES ON THE POLYURETHANE ELASTOMERS S. V. Riabov1, V. V. Boiko1, T.V. Dmitrieva1, L.V. Kobrina1, M.V. Gonchar2, T. M. Prokopiv2, A. E. Stepien3 1 Institute of Macromolecular Chemistry the National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Institute of Cell Biology, National Academy of Sciences of Ukraine, Lviv, Ukraine 3 Centre of Applied Biotechnology and Basic Sciences, Departament of Biotechnology, University of Rzeszow, Kolbuszowa, Poland |
| P54 | Modified urethaneureasilsesqiuoxanes L. P. Robota, V. G. Serov, Yu. V. Savelyev Institute of Macromolecular Chemistry of National Academy of Scainces of Ukraine, Kiev, Ukraine |
| P55 | HEAT CONDUCTIVITY OF POLYMER COMPOSITE MATERIAL BASED ON PENTON AND SILVER IODIDE (AgI) G. V. Rokitskaya, M. I. Shut, M. A. Rokitskiy, T. G. Sichkar National Pedagogical Dragomanov University, Kiev, Ukraine |
| P56 | FERROMAGNETIC COMPOSITE CELLULOSE-MAGNETITE R. Rotaru1, C. Peptu1, V. Harabagiu 1, M. Grigoras 2 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 National Institute of Research & Development for Technical Physics, Iasi, Romania |
| P57 | SUNLIGHT INDUCED PHOTOPOLYMERIZATION OF EPOXY-ACRYLATE INTERPENETRATING POLYMER NETWORKS T. F. Samoilenko, N. V. Iarova, H. I. Menzheres, O. O. Brovko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P58 | ANTICORROSIVE EPOXY COATING WITH POLYMER-SILICATE ADDITIVES D. S. Samoiliuk, T. V. Humenetskyy Lviv Polytechnic National University, Department of Polymer Processing, Lviv, Ukraine |
| P59 | Effect of PERMANENT magnetic field on patterns of synthesis and structure of cross-linked copolymer of polyvinylpyrrolidone V. Yo. Skorokhoda, Yu. Ya. Melnyk, N. B. Semenyuk, O. V. Suberlyak Lviv Polytechnic National University, Lviv, Ukraine |
| P60 | Сross-linked hydrogel copolymerS of polyvinylpyrrolidone as the matrices for the directed and controlled drugs release systems V. Skorokhoda, N. Semenyuk, G. Dudok, O. Suberlyak Lviv Polytechnic National University, Lviv, Ukraine |
| P61 | One-pot synthesis and characterization of double-network polyacrylamide/polysiloxane hydrogels O. V. Slisenko, I. M. Bei, V. L. Budzinska Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P62 | PRECISION SYNTHESIS OF TRIMETHYLENE CARBONATE AND LACTIDE COPOLYMERS VIA POLYMERIZATION WITH SUPPRESION OF TRANSESTERIFICATION M. Socka, A. Duda Centre of Molecular and Macromolecular Studies Polish Academy of Sciences, Lodz, Poland |
| P63 | STRUCTURE-PROPERTY RELATIONSHIPS FOR POROUS POLYAMIDOIMIDE-POLYURETHANE FILMS O. M. Starostenko1, O. P. Grigoryeva1, A. M. Fainleib1, V.V. Kremenitskiy2, V.M. Novichenko2 1 Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine 2 Technical center of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P64 | POLYURETHANE NANOCOMPOSITES CONTAINING REDUCED GRAPHENE OXIDE M. Strankowski1, E. Grzesiak2, B. Woźniak2 1 Polymer Technology Department, Chemical Faculty, Gdansk University of Technology, Gdansk, Poland 2Leather Industry Institute, Lodz, Poland |
| P65 | PROTIC OLIGOMERIC IONIC LIQUIDS A. V. Stryutsky, M. A. Gumenna, N. S. Klymenko, V. V. Shevchenko Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P66 | PROTONCONDUCTING ORGANIC-INORGANIC MEMBRANES FOR FUEL CELLS SYNTHESIZED BY SOL-GEL METHOD A. V. Stryutsky, M. A. Gumenna, N. S. Klymenko, V. V. Shevchenko Institute of Macromolecular Chemistry of the National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P67 | The influence of external factors and structural properties of ionic liquids based on polymeric quaternary salt of ammonium - derivatives of morpholine on their ionic conductivity O. S. Sverdlikovska, M. V. Burmistr State High Educational Institute «Ukrainian State University of Chemical Technology», Dnipropetrovsk, Ukraine |
| P68 | POLYPROPYLENE VERSUS COPOLYAMIDE: A COMPARATIVE STUDY OF COMPATIBILITY TOWARDS LAYERED SILICATES IN PRESET FORMULATIONS F. Tanasa, M. Zanoaga ”Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P69 | POLY(VINYLPYRROLIDONE) – A VERSATILE BIOMATERIAL FOR MEDICAL AND NON-MEDICAL APPLICATIONS M. Teodorescu “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P70 | SYNTHESIS AND CHARACTERIZATION OF CORE-FLUORINATED AROMATIC POLYMERS I. M. Tkachenko, A. V. Sidorenko, Ya. L. Kobzar, O. V. Shekera, V. V. Shevchenko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P71 | THE INFLUENCE OF THE BONDLINE THICKNESS ON THE EPOXY POLYMER PROPERTIES M. G. Tkalich, L. A. Gorbach, O. O. Brovko Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P72 | THE NANOSTRUCTURE OF POLYMER LAYERS FORMED ON A SOLID SURFACE BY ADSORPTION FROM BINARY AND TERNARY SOLUTIONS T. Todosijchuk, V. Chorna Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P73 | Environmentally friendly (bio)degradable xanthan based polyurethanes T. V. Travinskaya, A. N. Brykova, Yu. V. Savelyev Institute of Macromolecular Chemistry of National Academy of Sciences of Ukraine, Kiev, Ukraine |
| P74 | CHARACTERIZATION OF PEI-BASED GENE DELIVERY SYSTEMS C. M. Uritu, R. Ardeleanu, A. Coroaba, C. D. Varganici, L. Ursu, A. Nicolescu, M. Pinteala “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P75 | POST-MODIFICATION OF POLY(TRIPHENYLAMINE-VINYLENE)S: A WAY TO TUNE THEIR OPTICAL AND ELECTRONIC PROPERTIES L. Vacareanu1, A. M. Catargiu1, M. Grigoras1, B. Minaev2, E. Stromylo2 1 “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 Bogdan Khmelnitsky National University, Organic Chemistry Department, Cherkasy, Ukraine |
| P76 | THERMAL BEHAVIOR OF SEMIAROMATIC POLYIMIDES C.–D. Varganici1, D. Rosu1, C. Barbu–Mic2,3, L. Rosu1, D. Popovici2, C. Hulubei2, B. C. Simionescu1,3 1 Centre of Advanced Research in Bionanoconjugates and Biopolymers, ”Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 2 ”Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania 3”Gh. Asachi” Technical University of Iasi, Iasi, Romania |
| P77 | POLY(ETHYLENE GLYCOL) AND POLY(PROPYLENE GLYCOL)-CONTAINING AMINOFUNCTIONAL COPOLYESTERS FOR BIOMEDICAL APPLICATION A. S. Varvarenko1, A. Voronov2, N. Fihurka1, V. Samaryk1 , I. Tarnavchyk1, N. Nosova1, I. Dron1, M. Nagornyak1, M. Ferens1, S. Voronov1 1 Lviv Polytechnic National University, Organic Chemistry Department, Lviv, Ukraine 2 North Dakota State University, Coatings and Polymeric Materials Department, Fargo, ND, USA |
| P78 | COPOLYIMIDES BASED ON HEXAFLUOROISOPROPYLIDENE AND ALICYCLIC DIANHYDRIDES FOR GAS SEPARATION APPLICATION M. Wójtowicz1, A. Jankowski1, A. Wolińska-Grabczyk1, D. Popovici2, C. Hulubei2, M. Bruma2 1 Centre of Polymer and Carbon Materials, Polish Academy of Sciences, Zabrze, Poland 2 ”Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |
| P79 | CHEMICAL MODIFICATION OF POLYIMIDE MEMBRANES FOR CO2 SEPARATION M. Wójtowicz, E. Grabiec, A. Jankowski, A. Wolińska-Grabczyk Centre of Polymer and Carbon Materials, Polish Academy of Sciences, Zabrze, Poland |
| P80 | COORDINATION POLYMERS AND NETWORKS BUILD ON THE BASIS OF FLEXIBLE DICARBOXYLATE LIGANDS AND DIFFERENT METALLIC IONS M. F. Zaltariov, M. Cazacu, A. Vlad, S. Shova “Petru Poni” Institute of Macromolecular Chemistry, Iasi, Romania |